DIVISION 7 – THERMAL & MOISTURE PROTECTION

SECTION 07 92 00

JOINT SEALANTS

- GENERAL

  - SYSTEM DESCRIPTION

- This Section covers elastomeric and joint sealants, caulking compounds, and related accessories for exterior and interior joints where indicated on the Contract drawings and where required to obtain a weathertight structure.

  - SECTION INCLUDES

    - Exterior sealants.

    - Exterior EIFS sealants.

    - Exterior and interior polyether traffic sealants.

    - Interior sealants.

    - Interior USDA food contact sealants.

    - Interior sanitary silicone sealants.

    - Metal lap joint sealants.

    - Threshold and sheet metal bedding sealants.

    - Joint accessories.

  - RELATED SECTIONS

    - Section 03 31 00 – Structural Concrete.

    - Section 03 43 00 – Precast Structural Concrete.

    - Section 09 31 00 – Ceramic Tile.

    - Section 09 91 00 – Paints.

  - REFERENCES

    - ASTM International (ASTM):

      - ASTM C 510 - Standard Test Method for Staining and Colour Change of Single or Multi-component Joint Sealants.

      - ASTM C 719 - Standard Test Method for Adhesion and Cohesion of Elastomeric Joint Sealants under Cyclic Movement (Hockman Cycle).

      - ASTM C 794 - Standard Test Method for Adhesion-in-Peel of Elastomeric Joint Sealants.

      - ASTM C 920 - Standard Specification for Elastomeric Joint Sealants.

      - ASTM C 1087 - Standard Test Method for Determining Compatibility of Liquid- Applied Sealants with Accessories Used in Structural Glazing Systems.

      - ASTM C 1193 - Standard Guide for Use of Joint Sealants.

      - ASTM C 1248 - Standard Test Method for Staining of Porous Substrate by Joint Sealants.

      - ASTM D 412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers Tension.

      - ASTM D 679 - Methods of Testing and Tolerances for Certain Fine Staple Cotton Gray Goods.

      - ASTM D 816 - Standard Test Methods for Rubber Cements.

      - ASTM D 1002 - Standard Test Method for Apparent Shear Strength of Single-Lap-Joint Adhesively Bonded Metal Specimens by Tension Loading (Metal-to-Metal).

      - ASTM D 2203 - Standard Test Method for Staining from Sealants.

      - ASTM D 2240 - Standard Test Method for Rubber Property Durometer Hardness

    - American Concrete Institute (ACI);

- ACI 504R – Guide to Sealing Joints in Concrete Structures

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data: Manufacturer's data sheets on each product to be used, including:

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Installation methods.

    - Test Reports:

      - Submit results of laboratory pre-construction testing.

      - Submit results of field pre-construction testing.

      - Submit manufacturer's recommendations for joint preparation, priming, and joint accessory materials based on test results.

      - Submit manufacturer's recommended installation procedure modifications resulting from field adhesion tests.

    - Shop Drawings: Submit details to show installation and interface between sealants and adjacent work.

    - Selection Samples: For each finish product specified, two complete sets of colour charts for each sealant type for initial selection.

    - Verification Samples: For each finish product specified, two samples, standard cured colour samples for each sealant type illustrating selected colours.

    - Manufacturer's Certificate:

      - Certify products are suitable for intended use and products meet or exceed specified requirements.

      - Certify applicator is approved by manufacturer.

    - Qualifications Data:

      - Submit applicator's qualifications, including reference projects of similar scope and complexity, with current phone numbers and contact names of architects and owners for verification.

    - Manufacturer's Field Reports:

      - Indicate time present at project site.

      - Include observations; indicate compliance with manufacturer's installation instructions, and supplemental instructions provided to installers.

    - Operation and Maintenance Data:

      - Submit recommended inspection intervals.

      - Submit instructions for repairing and replacing failed sealant joints.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Minimum 10 year experience manufacturing similar products.

    - Applicator Qualifications:

      - Company specializing in performing work of this section with minimum three years documented experience, minimum three successfully completed projects of similar scope and complexity, and approved by manufacturer.

      - Designate one individual as project foreman who shall always be on site during installation.

    - Laboratory Pre-Construction Testing:

      - Test sealants, joint accessories, and joint substrates in accordance with the following, before starting work of this section:

        - Obtain samples of joint substrate products specified in other sections.

        - Adhesion: ASTM C 794 and ASTM C 719; determine surface preparation and required primer.

        - Compatibility: ASTM C 1087; determine materials forming joints and adjacent materials do not adversely affect sealant materials and do not affect sealant colour.

        - Staining: ASTM D 2203, ASTM C 510, or ASTM C 1248; determine sealants will not stain joint substrates.

      - Pre-construction testing is not required when sealant manufacturer can furnish data acceptable to Architect based on previous testing for materials matching those of the Work.

    - Field Pre-Construction Testing:

      - Test each elastomeric sealant and joint substrate in accordance with the following, before beginning work of this section:

        - Install sealants in field samples and mock-ups using joint preparation methods determined by laboratory pre-construction testing.

        - Remove existing sealant, clean joint, and install new sealant using manufacturer's recommended joint preparation methods.

        - Install field-test joints in inconspicuous location as approved by Architect].

        - Test Method: Manufacturer's standard field adhesion test to verify joint preparation and primer required to obtain optimum adhesion of sealants to joint substrate.

        - When test indicates sealant adhesion failure, modify joint preparation, primer, or both and retest until joint passes sealant adhesion test.

  - MOCK-UP

- Install sealants in mock-ups specified in other sections including sealant and joint accessories to illustrate installation quality and colour.

- Incorporate accepted Mockup as part of Work.

- Repair seal joint mock-ups used for field adhesion testing.

  - PRE-INSTALLATION MEETINGS

    - Convene minimum two weeks prior to starting work of this section.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver and store products in manufacturer's unopened packaging bearing the brand name and manufacturer's identification until ready for installation.

    - Store primers and sealants in cool dry location with ambient temperature below 25 degree C.

    - Handling: Handle materials to avoid damage.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

    - Optimal application temperature is 32 degree F (0 degree C) and rising.

      - Maintain sealant at room temperature before applying. If temperatures are below 32 degrees F (0 degrees C) contact manufacturer's customer service for application guidelines.

  - SEQUENCING

    - Schedule work so waterproofing, water repellents and preservative finishes are installed after sealants, unless sealant manufacturer approves otherwise in writing.

    - Ensure sealants are cured before covering with other materials.

    - Ensure that Work of this section are supplied to affected trades in time to prevent interruption of construction progress.

  - WARRANTY

- Provide manufacturer's signed standard limited warranty, against adhesive and cohesive failure of sealant and against infiltration of water and air through sealed joint for period of 1 year from date of completion.

      - Manufacturer's standard warranty covering sealant materials.

- PRODUCTS

- MANUFACTURER

- Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

- MATERIALS

    - POLYURETHANE JOINT SEALANTS

- Single-Component, Nonsag, Polyurethane Joint Sealant.

  - Compliance:

- ASTM C920 Type S, Grade NS, Class 25, use T1, M and A.

- ISO 11600, F 25 LM

- TT-S-00230C Class A, Type II

  - Physical Properties

- Shore A Hardness (ASTM D-2240):		       38 @21 days

- Elongation% (ISO8339):			            >173%

- Movement Capability:	                       ± 25%

- Service Temperature:					 -20 to 80ºC

- Time to Finish Curing:			            7 Days

- Working Time @25oC:					 120 minutes

Recommended products:

    - Vetoflex PU780, Manufacturer: Saudi Vetonit Company Ltd.

    - POLYSULPHIDE JOINT SEALANTS

- Multi-component, chemically curing, high-performance elastomeric polysulphide joint sealant.

  - Compliance:

- ASTM C920 Type S, Grade NS, Class 25, use T1, M and A.

- ISO 11600, Type F, Class 25 LM

- TT-S-00230C Class A, TypeII

  - Physical Properties

- Tensile Strength (ASTM D-412):		            ≥50

- Shore A Hardness (ASTM D-2240):		       P:15-25 NS:20-30

- Elongation% (ASTM D412):			       ≥250%

- Movement Capability:	                       ± 25%

- Service Temperature:					 -15 to +80ºC

- Tack Free Time (ASTM C697):				 ≤8 Hrs

- Time to Finish Curing:			            7 Days

- Working Time @25oC:					 120 minutes

Recommended products:

    - Vetoflex PS782, Manufacturer: Saudi Vetonit Company Ltd.

- ACCESSORIES

- Joint Cleaner: Non-corrosive and non-staining type, recommended by sealant manufacturer; compatible with joint forming materials.

- Primer: Non-staining type, recommended by sealant manufacturer to suit application.

- Joint Backing: Round polyethylene rod compatible with sealant; oversized 25 to 50 percent larger than joint width; recommended by sealant manufacturer to suit application

- Bond Breaker: Pressure sensitive tape recommended by sealant manufacturer to suit application.

- Masking tape: Non-staining, non-absorbent tape product compatible with joint sealants and adjacent joint surfaces.

- EXCUTION

  - EXAMINATION

    - Verify substrate surfaces and joint openings are ready to receive work.

      - Verify joint surfaces are clean and dry.

      - Ensure concrete surfaces are fully cured.

    - Report unsatisfactory conditions in writing to the Architect;

    - Do not proceed until unsatisfactory conditions are corrected.

  - PREPARATION

    - Prepare joints in accordance with ASTM C 1193 and manufacturer's instructions.

    - Clean joint surfaces to remove dirt, dust, oils, wax, paints, and other contamination capable of affecting primer and sealant bond.

    - Clean concrete joint surfaces to remove curing agents and form release agents.

    - Protect elements surrounding the Work of this section from damage or disfiguration. Apply masking tape to adjacent surfaces when required to prevent damage to finishes from sealant installation.

  - EXISTING WORK

    - Mechanically remove existing sealant.

    - Clean joint surfaces of residual sealant and other contaminates capable of affecting sealant bond to joint surface.

    - Allow joint surfaces to dry before installing new sealants.

  - SEALANT INSTALLATION

    - Install primer and sealants in accordance with ASTM C 1193 and manufacturer's instructions.

    - Install joint backing to maintain the following joint ratios:

      - Joints up to 13 mm Wide: 1:1 width to depth ratio.

      - Joints Greater than 13 mm Wide: 2:1 width to depth ratio; maximum 13 mm joint depth.

    - Install bond breaker where joint backing is not used.

    - Apply primer where required for sealant adhesion.

    - Install sealants immediately after joint preparation.

    - Install sealant free of air pockets, foreign embedded matter, ridges, and sags.

    - Tool exposed joint surface flat.

  - MANUFACTURER'S FIELD SERVICES

    - Require sealant manufacturer to be present at project site to:

      - Observe sealant mock-up installation and to issue reports of observations.

      - Conduct field pre-construction testing.

  - CLEANING

    - Remove masking tape. Clean adjacent surfaces soiled by sealant installation.

END OF SECTION