# SECTION 07 16 13

# POLYMER MODIFIED CEMENT WATERPROOFING

# PART 1 GENERAL

## SECTION INCLUDES

### This specification describes the coating of substrates with a non-vapor barrier, protective waterproofing, polymer-modified, Portland cement slurry. This waterproofing can be top coated with an aesthetic acrylic coating.

## RELATED SECTIONS

### Section 03 30 00 – Cast-in-Place Concrete.

### Section 03 40 00 – Precast Concrete.

## REFERENCES

### BS – British Standard

#### BS 6920-1 - Suitability of non-metallic materials and products for use in contact with water intended for human consumption with regard to their effect on the quality of the water Specification.

### EN – European Standard

#### EN 1062-3 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of liquid water permeability.

#### EN 1062-6 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of carbon dioxide permeability.

#### EN 1062-7 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of crack bridging properties.

#### EN 1062-11 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Methods of conditioning before testing.

#### EN 1081 - Resilient, laminate and modular multilayer floor coverings - Determination of the electrical resistance.

#### EN 1504-2 - Products and systems for the protection and repair of concrete structures - Definitions, requirements, quality control and evaluation of conformity - Part 2: Surface protection systems for concrete.

#### EN 1542 - Products and systems for the protection and repair of concrete structures - Test methods - Measurement of bond strength by pull-off.

#### EN 1770 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of the coefficient of thermal expansion.

#### EN ISO 2409 - Paints and varnishes. Cross-cut test.

#### EN ISO 2812-1 - Paints and varnishes. Determination of resistance to liquids Immersion in liquids other than water.

#### EN ISO 5470-1 - Rubber- or plastics-coated fabrics. Determination of abrasion resistance Taber abrader.

#### EN ISO 6272-1 - Paints and varnishes. Rapid-deformation (impact resistance) tests Falling-weight test, large-area indenter.

#### EN ISO 7783 - Paints and varnishes - Determination of water-vapor transmission properties - Cup method.

#### EN 12190 - Products and systems for the protection and repair of concrete structures - Test methods - Determination of compressive strength of repair mortar.

#### EN 12617-1 - Products and systems for the protection and repair of concrete structures. Test methods Determination of linear shrinkage for polymers and surface protection systems (SPS).

#### EN 13036-4 - Road and airfield surface characteristics. Test methods Method for measurement of slip/skid resistance of a surface: The pendulum test.

#### EN 13501-1 - Fire classification of construction products and building elements Classification using data from reaction to fire tests.

#### EN 13529 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of resistance to severe chemical attack.

#### EN 13578 - Products and systems for the protection and repair of concrete structures. Test method. Compatibility on wet concrete.

#### EN 13687-1 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of thermal compatibility Freeze-thaw cycling with de-icing salt immersion.

#### EN 13687-2 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of thermal compatibility Thunder-shower cycling (thermal shock).

#### EN 13687-3 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of thermal compatibility Thermal cycling without de-icing salt impact.

#### EN 13687-5 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of thermal compatibility Resistance to temperature shock.

#### EN 14891 - Liquid applied water impermeable products for use beneath ceramic tiling bonded with adhesives - Requirements, test methods, assessment and verification of constancy of performance, classification and marking.

### SASO – The Saudi Standards, Metrology and Quality

#### SASO-EN-1504-2 - Products and systems for the protection and repair of concrete structures - Definitions, requirements, quality control and evaluation of conformity - Surface protection systems for concrete.

## DEFINITIONS

### Cant-Strip: A beveled strip used under flashings to modify the angle at the point where the waterproofing membrane meets any vertical element.

### Elastomeric: A rubber like synthetic polymer that will stretch when pulled and will return quickly when released.

### Membrane: A flexible or semi-flexible waterproofing layer with the primary function of the exclusion of water.

### Reinforced Membrane: A waterproofing membrane reinforced with felts, mats, fabrics, or chopped fibers.

### Substrate: The surface upon which the waterproofing membrane is placed.

### Waterproofing: Treatment of a surface or structure to prevent the passage of water under hydrostatic pressure.

## SUBMITTALS

### The Contractor shall submit to the consultant, under the provisions of SECTION 013300, the following items for review and approval before commencing work:

#### Quality Control Program

##### The program shall cover items intended for shop inspection, field supervision and tests, as well as the procedures for carrying out the same, all-in accordance with SECTION 014500.

#### Product Data

##### Manufacturer’s catalogs, specifications, installation instructions, instructions for transporting, handling, and storing the materials and accessories to be used, and manufacturer’s quality control and quality assurance program related to the production, testing, and handling.

#### Certificates

##### Certificate of compliance stating that the materials used, and the installation procedures conform to all requirements of this Specification.

#### Samples

##### Samples shall be of 3 sets for all proposed materials.

#### Shop Drawings

##### Shop Drawings shall show all proposed work of this Section.

## QUALITY ASSURANCE

### Installer Qualifications: A firm that is approved by waterproofing manufacturer for installation of waterproofing required for this Project.

### Source Limitations: Obtain waterproofing materials and protection through one source from a single manufacturer to ensure compatibility. The source of each system component shall be confirmed.

### Pre-installation Conference: Conduct conference at Project site.

#### Review waterproofing requirements including surface preparation, substrate condition and pretreatment, minimum curing period, forecasted weather conditions, special details and installation procedures, testing and inspection procedures, protection, and repairs.

## HEALTH AND SAFETY CONSIDERTATIONS

### All works undertaken in relation to this Specification are to be completed in full accordance with the respective health and safety requirements established by the following:

#### United Arab Emirates, Kingdom of Saudi Arabia, rest of GCC and MENA region.

##### Legislation, Regulation, Standards and Codes.

#### Consultant Regulations

##### Standards, Contractual Conditions, and Health and Safety Systems.

#### Contractor

##### Health and Safety Standards and Systems as accepted by consultant.

### In the absence of any of the above, best accepted industry practice shall be employed throughout.

## JOB CONDATIONS

### Waterproofing work shall be proceeded only after substrate construction and penetrating work have been completed.

### Weather Conditions

#### Installation shall be started when existing and forecasted weather conditions are within the limits established by the membrane manufacturer.

### Personnel shall be warned against breathing of vapors and contact with skin and eyes.

### Keep flammable products away from spark or flame. Spark producing equipment shall not be used during application and until vapors have dissipated.

### Work area shall be maintained in a neat and workable condition. Empty cartons and rubbish shall be removed from the site daily.

## WARRANTY

### The Contractor shall provide a written 10-years material warranty from the manufacturer, and 5-years for installation, upon completion and acceptance of the installation.

## PERFORMANCE REQUIREMENTS

### General

#### Provide polymer modified cement waterproofing that complies with physical requirements indicated in the approved product data.

## DELIVERY, HANDLING AND STORAGE

### The Contractor shall deliver, handle and store equipment and material units in accordance with SECTIONS 016500 and 016600, as well as the following requirements:

#### All materials shall be delivered to site in manufacturer’s original containers and pallets. Each container and pallet shall include a packing list in a waterproof envelope.

#### The materials shall be checked against packing lists on delivery to the work site and shall be inspected for damage. Damaged materials shall be removed from site.

#### Each container and individual roll of waterproofing kit shall be labeled to show brand name, type of material, lot and shelf life, date of manufacture, batch number and instructions for storage and handling, if any.

#### All materials shall be adequately protected during shipment, loading, and unloading, storage and installation against incidental damage, sunlight and ultraviolet radiation, rain, and high temperature.

#### The materials shall be stored in dry, shaded, and covered areas. In open areas, the materials shall be covered with a heavy-duty sheet. The kit of waterproofing shall be stored on a smooth hard surface.

#### All necessary precautions shall be taken to prevent fire hazards in the storage area and during installations.

# PART 2 PRODUCTS

## GENERAL

### All goods and products covered by these Specifications shall be procured, when available, from an in-Kingdom of Saudi Arabia manufacturer.

### Unless otherwise indicated, materials shall conform to the requirements specified herein.

## MATERIALS

### Polymer modified cement waterproofing: shall be two coats with total wet film thickness of 2 mm as approved by Engineer. The polymer modified cement waterproofing should meet the following physical properties:

#### Abrasion resistance: Equivalent to 40 N/mm².

#### Resistance to positive water pressure: > 8 bar.

#### Resistance to negative water pressure: > 3 bar.

#### Static crack accommodation: > 1 mm.

#### Dynamic crack accommodation: 0.3 mm.

#### Bond strength: > 1 MPa after 28 days

#### Elongation: > 45%

#### Toxicity (BS 6920-1): Suitable for use with hot (up to 60°C) and cold water.

#### Manufacturer:

##### Saudi Vetonit Co. Ltd. (SAVETO), Vetoproof CM745.

##### Or approved equal.

### Auxiliary Materials

#### General: Furnish auxiliary materials recommended by waterproofing manufacturers for intended use and compatible with polymer modified cement waterproofing.

#### Fiberglass mesh: For total reinforcement of various waterproofing layers, with minimum weight thickness 65 g/m².

# PART 3 EXECUTION

## EXAMINATION

### Surfaces and site conditions, under which waterproofing is to be performed, shall be verified, and examined if ready to receive work. Work shall not be started until all defects have been corrected.

#### Verify that substrates to receive waterproofing are clean, sound, smooth, free of fins and sharp edges, loose and foreign matter, oil and grease and anything detrimental to waterproofing membrane. Pitted surfaces must be repaired before membrane installation.

#### Notify the Engineer in writing of anticipated problems using waterproofing over substrate.

#### Proceed with installation only after unsatisfactory conditions have been corrected.

## SUBSTRATE PREPARATION

### General

#### Preparation of the surface shall be done in accordance with sheet membrane manufacturer’s written instructions.

### Surfaces shall be clean and smooth, free of depressions, waves, projections, voids, holes (tie rod or rock pockets), spatters, ridges, and loose aggregates. Any contaminants shall be removed such as grease, oil, and wax.

#### All sharp protrusion shall be ground smooth and all hollows and honeycomb voids, and similar surface defects shall be filled with approved concrete fillers in accordance with SECTION 033100.

### The concrete surface shall be dry and shall be cleaned of all dust and debris.

### All concrete surfaces shall have a smooth finish. Broom finish concrete is not acceptable.

### Irregular construction joints and high spots shall be grind off to a suitable flush surface.

### Waterproofing shall not be applied to surfaces unacceptable to waterproofing manufacturer.

### Cracks shall be sealed using an approved sealant using depth to width ratio as recommended by waterproofing manufacturer.

- Coving to be done on all corners, joints and around penetrations.

- Coving: polymer modified cement mortar, or manufacturer approved fillet mortar compatible with waterproofing system. Coving is done in a concave profile (angle fillets of 45 degrees) shall be made at junctions, corners, and around pipe penetrations. Coving shall be smooth, fully bonded and free from cracks or voids, and be allowed to set sufficiently before waterproofing application. Coving to be done in internal and external areas such as toilets, kitchens, swimming pools, elevator shafts, parapet walls etc.

## MIXING

### Pour the liquid concentrate into a suitably sized mixing container.

### Commence mixing with a propeller agitator attached to a slow speed drill (300-500rpm).

### Gradually, add the powder component to the liquid part to avoid lump formation and mix for 2-4 minutes.

### Immediately after mixing, use the mix.

### Do not mix material more than the quantity that can use within the pot life.

### Keep mixing during the application.

## PRE-WETTING OF THE SUBSTRATE

### Thoroughly dampen the substrate surface with water using a brush roller or spray bottle.

### High porosity substrates will require more dampening than dense substrates.

### Do not apply the coating when the substrate is wet but allow the water to soak in until the substrate is just visibly damp before proceeding.

### Remove any excess water using a sponge.

## INSTALLATION

### Mix waterproof lining material in proportions recommended by manufacturer.

### Apply waterproof lining material in quantities as per manufacturer's specifications and recommendations.

### Cavity Fill:

#### At cleaned and prepared faulty construction joints, cracks, form tie, nail and bug holes, fill voids with patching compound in mortar consistency flush to surface. Leave rough surface finish for subsequent waterproofing material to bond.

### Floor/wall and corner joints:

#### Install (rounded) coves 5 cm x 5 cm with patching compound in mortar consistency. Leave rough surface finish for subsequent waterproof lining material to bond.

### Horizontal and vertical surfaces – damp proofing / subject to hydrostatic pressure:

#### Apply the first coat of waterproof lining material at a wet film thickness of 1mm.

##### Apply by masonry brush, steel trowel or appropriate compressed-air spray equipment. Back-trowel application to uniform thickness if applied with spray equipment.

##### During application, take care of filling the imperfections such as blowholes.

##### If not, fill them while the coating is still in fluid status by using a dry sponge. If the coating dried before finding these imperfections, fill them using fresh material.

##### The exact drying time will depend on surface temperature, relative humidity, and air movement.

##### High temperatures and/or low humidity will reduce the drying time. This can vary from 1 to 16 hours. Leave the first coat to dry until firm and non-markable to the touch.

##### There is no maximum time between coats; however, the surface may need cleaning with water before applying the second coat to remove potential contamination.

#### Apply the second coat of waterproof lining material at a wet film thickness of 1mm after first coat has sufficiently hardened (approximately 2 to 4 hours).

##### Pre-dampening of the surface is not necessary before applying the second coat.

##### Apply by masonry brush, steel trowel or appropriate air spray equipment. Surface finish shall be troweled smooth, or dense, glazed appearance if sprayed, showing little indentations from air pressure (orange skin).

##### For total reinforcement of waterproof lining material use fiberglass mesh, especially to weak areas such as vertical and horizontal points meeting.

##### However, the polymer modified cement waterproofing is self-curing; protect the freshly applied coating from rain and strong wind until it becomes firm to the touch.

## CURING

### Allow the waterproofing to cure for at least 7 days before commissioning, or as per manufacturer's instructions.

## PROTECTION, CLEANING AND OTHER FOLLOWING FINISHES

### General

#### Areas with waterproofing shall be protected either with screed or protection board at the end of a working day. No storage of materials or traffic shall be allowed on the unprotected areas with waterproof lining material.

#### Immediately following application, clean all tools and equipment with clean water. Hardened material can be removed by mechanical means.

#### Remove left over materials and any foreign material resulting from the work from the site.

- Where tiling to be done on waterproofed surfaces, always use a polymer modified cement adhesive complying with BS EN 12004 class C2 range.

- Where waterproofing is required for walls, plaster is applied first and cured. Never apply the cementitious waterproof before the plastering.

# END OF SECTION