# SECTION 07 56 00

# FLUID-APPLIED ROOFING

# PART 1 GENERAL

## SECTION INCLUDES

### This specification describes a cold-fluid-applied acrylic/polyurethane hybrid roofing/waterproofing system on structural concrete, cement, cover board, metal corrugated sheet, sprayed polyurethane foam or other substrates.

## RELATED SECTIONS

### Section 03 30 00 – Cast-in-Place Concrete.

### Section 03 40 00 – Precast Concrete.

### Section 06 16 00 – Sheeting.

### Section 07 60 00 – Flashing and Sheet Metal.

### Section 07 92 13 – Elastomeric Joint Sealants.

### Section 07 57 13 – Sprayed Polyurethane Foam Roofing.

### Section 21 14 25 – Roof Drains.

## REFERENCES

### EN – European Standard

#### EN 1062-3 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of liquid water permeability.

#### EN 1062-6 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of carbon dioxide permeability.

#### EN 1062-7 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Determination of crack bridging properties.

#### EN 1062-11 - Paints and varnishes. Coating materials and coating systems for exterior masonry and concrete Methods of conditioning before testing.

#### EN 1504-2 - Products and systems for the protection and repair of concrete structures - Definitions, requirements, quality control and evaluation of conformity - Part 2: Surface protection systems for concrete.

#### EN 1542 - Products and systems for the protection and repair of concrete structures - Test methods - Measurement of bond strength by pull-off.

#### EN 1770 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of the coefficient of thermal expansion.

#### EN ISO 5470-1 - Rubber- or plastics-coated fabrics. Determination of abrasion resistance Taber abrader.

#### EN ISO 6272-1 - Paints and varnishes. Rapid-deformation (impact resistance) tests Falling-weight test, large-area indenter.

#### EN ISO 7783 - Paints and varnishes - Determination of water-vapor transmission properties - Cup method.

#### EN 13501-1 - Fire classification of construction products and building elements Classification using data from reaction to fire tests.

#### EN 13529 - Products and systems for the protection and repair of concrete structures. Test methods. Determination of resistance to severe chemical attack.

### SASO – The Saudi Standards, Metrology and Quality

#### SASO-EN-1504-2 - Products and systems for the protection and repair of concrete structures - Definitions, requirements, quality control and evaluation of conformity - Surface protection systems for concrete.

## DEFINITIONS

### Cant-Strip: A beveled strip used under flashings to modify the angle at the point where the waterproofing membrane meets any vertical element.

### Elastomeric: A rubber like synthetic polymer that will stretch when pulled and will return quickly when released.

### Membrane: A flexible or semi-flexible waterproofing layer with the primary function of the exclusion of water.

### Reinforced Membrane: A waterproofing membrane reinforced with felts, mats, fabrics, or chopped fibers.

### Substrate: The surface upon which the waterproofing membrane is placed.

### Waterproofing: Treatment of a surface or structure to prevent the passage of water under hydrostatic pressure.

## SUBMITTALS

### The Contractor shall submit to the consultant, under the provisions of SECTION 013300, the following items for review and approval before commencing work:

#### Quality Control Program

##### The program shall cover items intended for shop inspection, field supervision and tests, as well as the procedures for carrying out the same, all-in accordance with SECTION 014500.

#### Product Data

##### Manufacturer’s catalogs, specifications, installation instructions, instructions for transporting, handling, and storing the materials and accessories to be used, and manufacturer’s quality control and quality assurance program related to the production, testing, and handling.

#### Certificates

##### Certificate of compliance stating that the materials used, and the installation procedures conform to all requirements of this Specification.

#### Samples

##### Samples shall be of 3 sets for all proposed materials.

#### Shop Drawings

##### Shop Drawings shall show all proposed work of this Section.

## QUALITY ASSURANCE

### Installer Qualifications: A firm that is approved by waterproofing manufacturer for installation of waterproofing required for this Project.

### Source Limitations: Obtain waterproofing materials and protection through one source from a single manufacturer to ensure compatibility. The source of each system component shall be confirmed.

### Pre-installation Conference: Conduct conference at Project site.

#### Review waterproofing requirements including surface preparation, substrate condition and pretreatment, minimum curing period, forecasted weather conditions, special details and installation procedures, testing and inspection procedures, protection, and repairs.

## HEALTH AND SAFETY CONSIDERTATIONS

### All works undertaken in relation to this Specification are to be completed in full accordance with the respective health and safety requirements established by the following:

#### United Arab Emirates

##### Legislation, Regulation, Standards and Codes.

#### Consultant Regulations

##### Standards, Contractual Conditions, and Health and Safety Systems.

#### Contractor

##### Health and Safety Standards and Systems as accepted by consultant.

### In the absence of any of the above, the best accepted industry practice shall be employed throughout.

## JOB CONDATIONS

### Waterproofing work shall be proceeded only after substrate construction and penetrating work have been completed.

### Weather Conditions

#### Installation shall be started when existing and forecasted weather conditions are within the limits established by the membrane manufacturer.

### Personnel shall be warned against breathing vapors and contact with skin and eyes.

### Keep flammable products away from sparks or flames. Spark producing equipment shall not be used during application and until vapors have dissipated.

### The work area shall be maintained in a neat and workable condition. Empty cartons and rubbish shall be removed from the site daily.

## WARRANTY

### The Contractor shall provide a written 10-years material warranty from the manufacturer, and 5-years for installation, upon completion and acceptance of the installation.

## PERFORMANCE REQUIREMENTS

### General

#### Provide a cold-fluid-applied acrylic/polyurethane roofing/waterproofing that complies with physical requirements indicated in the approved product data.

## DELIVERY, HANDLING AND STORAGE

### The Contractor shall deliver, handle and store equipment and material units in accordance with SECTIONS 016500 and 016600, as well as the following requirements:

#### All materials shall be delivered to site in manufacturer’s original containers and pallets. Each container and pallet shall include a packing list in a waterproof envelope.

#### The materials shall be checked against packing lists on delivery to the work site and shall be inspected for damage. Damaged materials shall be removed from site.

#### Each container and individual roll of waterproofing kit shall be labeled to show brand name, type of material, lot and shelf life, date of manufacture, batch number and instructions for storage and handling, if any.

#### All materials shall be adequately protected during shipment, loading, and unloading, storage and installation against incidental damage, sunlight and ultraviolet radiation, rain, and high temperature.

#### The materials shall be stored in dry, shaded, and covered areas. In open areas, the materials shall be covered with a heavy-duty sheet. The kit of waterproofing shall be stored on a smooth hard surface.

#### All necessary precautions shall be taken to prevent fire hazards in the storage area and during installations.

# PART 2 PRODUCTS

## GENERAL

### All goods and products covered by these Specifications shall be procured, when available, from an in-Kingdom of Saudi Arabia manufacturer.

### Unless otherwise indicated, materials shall conform to the requirements specified herein.

## ROOFING SYSTEM

### Fluid-Applied Roofing System: Acrylic/Polyurethane Hybrid:

#### Primer: Water repellant and anti-chloride primer.

#### Base Layer: acrylic/polyurethane hybrid roofing/waterproofing membrane, wet film thickness 1.0 mm.

#### Membrane Reinforcement: non-woven, needle-punched polyester fleece, 100 g/m².

#### Top Layer #1: acrylic/polyurethane hybrid roofing/waterproofing membrane, wet film thickness 0.5 mm.

#### Top Layer #2: acrylic/polyurethane hybrid roofing/waterproofing membrane, wet film thickness 0.5 mm.

## MATERIALS

### Acrylic/Polyurethane Hybrid Roofing/Waterproofing Membrane: shall be three coats with total wet film thickness of 2.0 mm as approved by Engineer. The acrylic/polyurethane hybrid membrane should meet the following physical properties:

#### Resistance to Positive Water Pressure: > 1.5 bar.

#### Bond Strength: > 0.35 MPa.

#### Tensile Strength: > 2.50 MPa.

#### Elongation at Break: > 300 %.

#### Static Crack Accommodation: > 4 mm.

#### Dynamic Crack Accommodation: > 1 mm.

#### Weathering Resistance: 2000 hours – no change.

#### Solar Reflective Index: > 100.

#### Manufacturer:

##### Saudi Vetonit Co. Ltd. (SAVETO), Saveto Cool Top.

##### Or approved equal.

### Auxiliary Materials

#### General: Furnish auxiliary materials recommended by waterproofing manufacturer for intended use and compatible with acrylic/polyurethane hybrid roofing/waterproofing membrane.

#### Primer: Concrete, roof cover boards and sealing cementitious and gypsum-based substrates shall be primed with Vetoprime AP443.

#### Membrane Reinforcement - Polyester: Reinforcement for the roofing/waterproofing system shall be non-woven, needle-punched polyester fleece specifically designed to provide greater impact resistance and greater resistance to excessive thermal and structural movement while maintaining elasticity and membrane film integrity, 100 g/m².

# PART 3 EXECUTION

## EXAMINATION

### Surfaces and site conditions, under which waterproofing is to be performed, shall be verified, and examined if ready to receive work. Work shall not be started until all defects have been corrected.

#### Verify that substrates to receive waterproofing are clean, sound, smooth, free of fins and sharp edges, loose and foreign matter, oil and grease and anything detrimental to waterproofing membrane. Pitted surfaces must be repaired before membrane installation.

#### Notify the Engineer in writing of anticipated problems using waterproofing over substrate.

#### Proceed with installation only after unsatisfactory conditions have been corrected.

## SUBSTRATE PREPARATION

### General

#### Preparation of the surface shall be done in accordance with the waterproofing membrane manufacturer’s written instructions.

#### Surfaces shall be clean and smooth, free of depressions, waves, projections, voids, holes (tie rod or rock pockets), spatters, ridges, and loose aggregates. Any contaminants shall be removed such as grease, oil, and wax.

#### All sharp protrusion shall be ground smooth and all hollows and honeycomb voids, and similar surface defects shall be filled.

#### The surface shall be dry and shall be cleaned of all dust and debris.

#### Cracks shall be sealed using an approved sealant as recommended by the waterproofing manufacturer.

## PRIMING

### Prime porous surfaces with penetrating sealer water repellent and hardener primer by brush or roll and allow it to cure as per the manufacturer’s instructions.

## INSTALLATION

### Apply the base coat of waterproofing membrane by brush or roll and topped by a polyester fleece reinforcement membrane on the wet coating and allow it to cure as per the manufacturer’s instructions.

### Apply the first topcoat of waterproofing membrane with a brush or roll and allow it to cure as per the manufacturer’s instructions.

### Apply the second topcoat of waterproofing membrane with a brush or roll and allow it to cure as per the manufacturer’s instructions.

### Apply the last topcoat of colored acrylic membrane with a brush or roll and allow it to cure as per the manufacturer’s instructions.

## CURING

### Allow the waterproofing to cure for at least 7 days before commissioning, or as per the manufacturer’s instructions.

## PROTECTION AND CLEANING

### No storage of materials or traffic shall be allowed in unprotected areas with waterproofing material.

### Immediately following application, clean all tools and equipment with clean water. Hardened material can be removed by mechanical means.

### Remove leftover materials and any foreign material resulting from the work from the site.

# END OF SECTION