DIVISION 09 - FINISHES

SECTION 07 13 53

ELASTOMERIC SHEET WATERPROOFING

# PART 1 GENERAL

## SECTION INCLUDES

- This specification describes polyvinyl chloride (PVC) single ply waterproofing membrane for lining of drinking water tanks.

## RELATED SECTIONS

- Section 03 30 00 –Cast-in-Place Concrete.

- Section 03 31 00 – Structural Concrete.

- Section 03 15 13 – Water stops.

- Section 04 20 00 – Unit Masonry.

- Section 07 92 00 – Joint Sealants.

## DEFINITIONS

### Cant Strip: A beveled strip used under flashings to modify the angle at the point where the waterproofing membrane meets any vertical element.

### Elastomeric: A rubber-like synthetic polymer that will stretch when pulled and will return quickly when released.

### Flashing: The system is used to seal membrane edges at walls, expansion joints, drains, gravel stops, and other places where the membrane is interrupted or terminated. Base flashing covers the edges of the membrane. Cap or counterflashing shields the upper edges of the base flashing.

### Loose-Laid Membrane: A ballasted roofing membrane that is attached to the substrate only at the edges and penetrations through the roof.

### Membrane: A flexible or semi-flexible waterproofing layer with the primary function of the exclusion of water.

### Reinforced Membrane: A waterproofing membrane reinforced with felts, mats, fabrics, or chopped fibers.

### Substrate: The surface upon which the waterproofing membrane is placed.

### Thermoplastic: Becoming soft when heated and hard when cooled.

### Waterproofing: Treatment of a surface or structure to prevent the passage of water under hydrostatic pressure.

## REFERENCES

- BS – British Standard

- BS 6920-1 - Suitability of non-metallic materials and products for use in contact with water intended for human consumption regarding their effect on the quality of the water Specification.

- ANSI- American National Standards Institute

- NSF/ANSI 61: Drinking Water System Components – Health Effects

- ASTM- American Society for Testing and Materials

- ASTM D4551 - Standard Specification for Poly (Vinyl Chloride) (PVC) Plastic Flexible Concealed Water-Containment Membrane.

## SUBMITTALS

### The Contractor shall submit to the consultant, under the provisions of SECTION 013300, the following items for review and approval before commencing work:

#### Quality Control Program

##### The program shall cover items intended for shop inspection, field supervision and tests, as well as the procedures for carrying out the same, all-in accordance with SECTION 014500.

#### Product Data

- Manufacturer’s catalogs, specifications, installation instructions, instructions for transporting, handling, and storing the materials and accessories to be used.

#### Certificates

##### Certificate of compliance stating that the materials used, and the installation procedures conform to all requirements of this Specification.

#### Samples

##### Samples shall be submitted for proposed materials.

#### Shop Drawings

##### Shop Drawings shall show all proposed work of this Section.

## QUALITY ASSURANCE

### Installer Qualifications: A firm that is approved by manufacturer for installation is required for this Project.

### Pre-installation Conference: Conduct conference at Project site.

#### Review requirements including surface preparation, substrate condition and pretreatment, minimum curing period, forecasted weather conditions, special details and installation procedures, testing and inspection procedures, protection, and repairs.

## HEALTH AND SAFETY CONSIDERTATIONS

### All works undertaken in relation to this Specification are to be completed in full accordance with the respective health and safety requirements established by the following:

#### Consultant Regulations

##### Standards, Contractual Conditions, and Health and Safety Systems.

#### Contractor

##### Health and Safety Standards and Systems as accepted by consultant.

### In the absence of any of the above, the best accepted industry practice shall be employed throughout.

## JOB CONDATIONS

### Weather Conditions

#### Installation shall be started when existing and forecasted weather conditions are within the limits established by the membrane manufacturer.

### The work area shall be maintained in a neat and workable condition. Empty cartons and rubbish shall be removed from the site daily.

- Personnel shall be warned against breathing vapors and contact with skin and eyes.

- Keep flammable products away from sparks or flames. Spark producing equipment shall not be used during application and until vapors have dissipated.

## WARRANTY

- The Contractor shall provide a written 5-years material warranty from the manufacturer, and 5-years for installation, upon completion and acceptance of the installation.

## PERFORMANCE REQUIREMENTS

### General

- Provide a non-toxic polyvinyl chloride (PVC) single ply waterproofing membrane for concrete tanks and reservoirs used for the containment of potable water.

## DELIVERY, HANDLING AND STORAGE

### The Contractor shall deliver, handle and store equipment and material units in accordance with SECTIONS 016500 and 016600, as well as the following requirements:

#### All materials shall be delivered to site in manufacturer’s original containers and pallets.

#### The materials shall be checked against packing lists on delivery to the work site and shall be inspected for damage. Damaged materials shall be removed from site.

#### All materials shall be adequately protected during shipment, loading, and unloading, storage and installation against incidental damage, sunlight and ultraviolet radiation, rain, and high temperature.

#### The materials shall be stored in dry, shaded, and covered areas. In open areas, the materials shall be covered with a heavy-duty sheet. The kit of waterproofing shall be stored on a smooth hard surface.

#### All necessary precautions shall be taken to prevent fire hazards in the storage area and during installations.

# PART 2 PRODUCTS

2.01 GENERAL

- All goods and products covered by these Specifications shall be procured, which available, from an in‐Kingdom manufacturer.  Procurement of all goods and products manufactured out‐of‐Kingdom must be approved by The Consulting Entity.

  - ANUFACTURERS

- Acceptable Manufacturer: Waterproofing & Wrapping Products Co. Ltd. (INSUWRAP), P.O. Box 17579, Riyadh 11494 Saudi Arabia. Tel: 03 857 6790.  Fax: 03 858 7607.  Web: www.insuwrap.com

- Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

## MATERIALS

### POLYVINYL CHLORIDE (PVC) SINGLE PLY WATERPROOFING MEMBRANE

### Non-toxic thermoplastic polyvinyl chloride (PVC) single ply waterproofing membrane Lining of concrete tanks and reservoirs used for the containment of potable water. with thickness of 1.50 mm, reinforced with polyester mesh, manufactured following highest international standards offering high physical properties and long-term durability.

### Technical Performance Requirements:

### Thickness (mm): 1.5 mm

### Tensile Strength (ASTM D 412 Method A): 15 KN/m

### Tenile strength @100% elongation (ASTM D 412 Method A): > 10 KN/m

### Elongation @ Break (ASTM D 412 Method A): > 300%

### Tear Resistance (ASTM D751 A-grab method): 50 KN/m

### Micro-organism resistance (ASTM D 4551 annex A1): Pass

### Puncture resistance (ASTM D34551 annix A2): Pass

### Indentation resistance (ASTM D4551 annex A3): Pass

### Folding resistance (ASTM D4551 annex A4): Pass

### Distilled H2O resistance (ASTM D543, Procedure 1): 0.3%

### Soapy H2O resistance (ASTM D543, Procedure 1): 0.5%

### Alkali resistance (ASTM D543, Procedure 1): Pass

### Hydrostatic pressure test (ASTM D4551 annex A5): Pass

### Shrinkage (ASTM D1204): 1%

### Volatile loss (ASTM D1203): 0.5%

### Fire Class (ASTM E108): Pass (Class B)

- has NSF/ANSI 61 approval for suitability for use with drinking water.

- Pass the requirements of ASTM D4551.

### Basis of Design Product: Subject to compliance with requirements, “INSUWRAP PVC 1500 LNTR” manufactured by Insuwrap.

### AUXILIARY MATERIALS

#### General: Furnish auxiliary materials recommended by the waterproofing manufacturer for intended use and compatible with sheet waterproofing.

# PART 3 EXECUTION

## 3.01 EXAMINATION

### Surfaces and site conditions, under which membrane waterproofing is to be performed, shall be verified, and examined if ready to receive work. Work shall not be started until all defects have been corrected.

#### Verify that substrates to receive waterproofing are clean, sound, smooth, free of fins and sharp edges, loose and foreign matter, oil and grease, and anything detrimental to the waterproofing membrane. Pitted surfaces must be repaired before membrane installation.

#### Notify the Engineer in writing of anticipated problems using waterproofing over substrate.

#### Proceed with installation only after unsatisfactory conditions have been corrected.

## SUBSTRATE PREPARATION

    - Internal concrete surface should be smooth, clean and free from sharp projections otherwise a protection layer (non-woven polyester 140 g/m2) must be used to receive PVC membranes.

## INSTALLATION

- General

Membrane waterproofing shall be installed according to the manufacturer’s instructions and according to the following requirements:

- Horizontal Surface

- Apply INSUWRAP PVC liner loose laid for horizontal areas with 50 mm overlaps by using hot air welding technique.

- Horizontal PVC membranes must be installed to 300 mm height on the vertical walls to enable the welder to join the horizontal membranes at the corners. The membranes will be mechanically fixed with PVC coated angles or strips properly and it will be welded to the vertical PVC membranes.

- Vertical Surface

- Apply INSUWRAP PVC liner vertically by mechanical fixation using aluminum strips or PVC coated metal strips (30 mm width with smooth edges) fixed by fasteners at the end of the lining membranes or each roll.

- Overlaps (50 mm) will be welded homogeneously using hot air welding technique.

- PVC coated galvanized metal strips or Aluminum flashing (50 mm width) with one bend (10 mm) shall be provided on the termination of the lining membranes. Non-toxic sealant will be filled on the top of the flashing.

- flanges, ladder etc., passing through junctions must be completely watertight using preformed collars fully bonded/sealed to the mentioned fittings. Dressings can be made at the site using the same PVC liner.

  - FIELD QUALITY CONTROL

- General

The completed membrane shall be examined for defective or damaged areas before installing the protection course and shall be repaired or replaced according to the written instructions of the manufacturer.

- Flood Test

- The Contractor shall provide temporary construction and materials for testing.

- Before applying the protection layer, all horizontal applications shall be flood-tested with a minimum of 50 mm head of clean water for 72 hours.

- If a leak is found, water shall be removed, and leaking areas shall be repaired with new waterproofing materials as the Consultant directs.

- Flood testing shall be repeated. When the area is proven watertight, water shall be drained, and the dam shall be removed.

- Vacuum Test.

- Needle Test.

- Pressure Gauge Test.

END OF SECTION