# SECTION 07 13 54

# THERMOPLASTIC SHEET WATERPROOFING

# PART 1 GENERAL

## SECTION INCLUDES

### Polyvinyl Chloride (PVC) sheet waterproofing for underground structures.

## RELATED REQUIREMENTS

### Section 03 15 13 – Water stops.

### Section 03 30 00 – Cast-in-Place Concrete.

### Section 03 31 00 – Structural Concrete.

### Section 04 20 00 – Unit Masonry.

### Section 07 92 00 – Joint Sealants.

## DEFINITIONS

### Cant Strip: A beveled strip used under flashings to modify the angle at the point where the waterproofing membrane meets any vertical element.

### Elastomeric: A rubber-like synthetic polymer that will stretch when pulled and will return quickly when released.

### Fabric: A woven or non-woven cloth of organic or inorganic filaments, threads, or yarns.

### Flashing: The system is used to seal membrane edges at walls, expansion joints, drains, gravel stops, and other places where the membrane is interrupted or terminated. Base flashing covers the edges of the membrane. Cap or counterflashing shields the upper edges of the base flashing.

### Loose-Laid Membrane: A ballasted roofing membrane that is attached to the substrate only at the edges and penetrations through the roof.

### Membrane: A flexible or semi-flexible waterproofing layer with the primary function of the exclusion of water.

### Reinforced Membrane: A waterproofing membrane reinforced with felts, mats, fabrics, or chopped fibers.

### Substrate: The surface upon which the waterproofing membrane is placed.

### Thermoplastic: Becoming soft when heated and hard when cooled.

### Waterproofing: Treatment of a surface or structure to prevent the passage of water under hydrostatic pressure.

## REFERENCE STANDARDS

### American Society for Testing and Materials (ASTM):

#### ASTM D543 - Standard Practices for Evaluating the Resistance of Plastics to Chemical Reagents.

#### ASTM D4439 - Standard Terminology for Geosynthetics.

#### ASTM D4551 - Standard Specification for Poly (Vinyl Chloride) (PVC) Plastic Flexible Concealed Water-Containment Membrane.

#### ASTM D7176 - Standard Specification for Non-Reinforced Polyvinyl Chloride (PVC) Geomembranes Used in Buried Applications.

## SUBMITTALS

### Product Data:

#### Manufacturer’s catalogs, specifications, installation instructions, instructions for transporting, handling, and storing the materials and accessories to be used, and manufacturer’s quality control and quality assurance program related to the production, testing, and handling.

### Shop Drawing:

#### Shop Drawings shall show all proposed work of this Section.

### Samples:

#### Samples shall be of 3 sets for all proposed materials.

### Certificate:

#### Certificate of compliance stating that the materials used, and the installation procedures conform to all requirements of this Specification.

## QUALITY ASSURANCE

### Qualifications:

#### Manufacturers: Shall be ISO 9001 certified.

#### Approved by a waterproofing manufacturer for the installation of waterproofing required and on at least three projects equal in scope to this work and specializing in performing the work of this section with a minimum of three years of documented experience.

### Source Limitations: Obtain waterproofing materials and protection through one source from a single manufacturer to ensure compatibility. The source of each system component shall be confirmed.

### Pre-installation Conference: Conduct a conference at the Project site.

#### Review waterproofing requirements including surface preparation, substrate condition and pretreatment, minimum curing period, forecasted weather conditions, special details and installation procedures, testing and inspection procedures, protection, and repairs.

## DELIVERY, HANDLING AND STORAGE

### All materials shall be delivered to the site in the manufacturer’s original containers and pallets. Each container and pallet shall include a packing list in a waterproof envelope.

### The materials shall be checked against packing lists on delivery to the work site and shall be inspected for damage. Damaged materials shall be removed from the site.

### Each container and individual roll of membrane sheet shall be labeled to show the brand name, type of material, lot and shelf life, date of manufacture, batch number, and instructions for storage and handling, if any.

### All materials shall be adequately protected during shipment, loading, unloading, storage, and installation against incidental damage, sunlight and ultraviolet radiation, rain, and high temperature.

### The materials shall be stored in dry, shaded, and covered areas. In open areas, the materials shall be covered with a heavy-duty PVC sheet. The rolls of membrane shall be stored on a smooth hard surface.

### All necessary precautions shall be taken to prevent fire hazards in the storage area and during installations.

## SITE CONDITIONS

### Waterproofing work shall proceed only after substrate construction and penetrating work have been completed.

### Weather Conditions:

#### Installation shall be started when existing and forecasted weather conditions are within the limits established by the membrane manufacturer.

### Personnel shall be warned against breathing vapors and contact with skin and eyes.

### Keep flammable products away from sparks or flames. Spark-producing equipment shall not be used during application and until vapors have dissipated.

### The work area shall be maintained in a neat and workable condition. Empty cartons and rubbish shall be removed from the site daily.

## WARRANTY

### The Contractor shall provide a written ten-year material warranty from the manufacturer, and five years for installation, upon completion and acceptance of the installation.

# PART 2 PRODUCTS

## MANUFACTURERS

### Manufacturer List:

#### INSUWRAP.

#### Or equally approved.

## MATERIALS

### Thermoplastic single-ply polyvinyl chloride (PVC) waterproofing membrane for underground structures meets the following properties:

#### Thickness: 1.5 mm.

#### Tensile Strength at Break: ≥ 15 kN/m.

#### Tensile Elongation: ≥ 250 %.

#### Tensile Modulus at 100 %: ≥ 10 kN/m.

#### Tear Strength: ≥ 50.

#### Dimensional Stability: ≤ 3 %.

#### Low-Temperature Impact: - 29°C Pass.

#### Water Extraction: ≤ 0.15 % loss.

#### Volatile Loss: ≤ 0.15 % loss.

#### Soil Burial Break Strength: ≤ 2.5 %.

#### Soil Burial Elongation: ≤ 12 %.

#### Soil Burial Modulus at 100 %: ≤ 17 %.

#### Hydrostatic Resistance: ≥ 290 KPa.

#### Minimum Average Molecular Weight: 400.

#### Puncture Resistance: Pass.

#### Seam Strength: Pass.

#### Fire Test: Class B.

#### Products:

##### Insuwrap PVC 1500 TNL.

##### Or equivalent.

### Auxiliary Materials

#### General: Furnish auxiliary materials recommended by the waterproofing manufacturer for intended use and compatible with sheet waterproofing.

# PART 3 EXECUTION

## EXAMINATION

### Surfaces and site conditions, under which membrane waterproofing is to be performed, shall be verified, and examined if ready to receive work. Work shall not be started until all defects have been corrected.

#### Verify that substrates to receive waterproofing are clean, sound, smooth, free of fins and sharp edges, loose and foreign matter, oil and grease, and anything detrimental to the waterproofing membrane. Pitted surfaces must be repaired before membrane installation.

#### Notify the Engineer in writing of anticipated problems using waterproofing over substrate.

#### Proceed with installation only after unsatisfactory conditions have been corrected.

## PREPARATION

### General

#### Preparation of the surface shall be done according to the sheet membrane manufacturer’s written instructions.

### Surfaces shall be clean and smooth, free of depressions, waves, projections, voids, holes (tie rod or rock pockets), spatters, ridges, and loose aggregates. Any contaminants shall be removed such as grease, oil, and wax.

#### All sharp protrusion shall be ground smooth and all hollow honeycomb voids, and similar surface defects shall be filled with approved concrete fillers by SECTION 033100.

### The concrete surface shall be dry and shall be cleaned of all dust and debris.

### All concrete surfaces shall have a smooth finish. Broom finish concrete is not acceptable.

### Irregular construction joints and high spots shall be grinding off to a suitable flush surface.

### Waterproofing shall not be applied to surfaces unacceptable to membrane manufacturer.

### Cracks shall be sealed using an approved sealant using the depth-to-width ratio as recommended by the sealant manufacturer.

## INSTALLATION

### General

#### Membrane waterproofing shall be installed according to the manufacturer’s instructions and according to the following requirements:

##### Typical installation details shall be by standard drawing, “Membrane Waterproofing for Concrete Structures.”

##### A minimum lap of 75 mm shall be provided at the edges and 150 mm at the ends between the adjacent sheets.

##### One layer of membrane shall be laid directly over the horizontal surface of blinding under the footings and a layer of 25 mm thick sand/cement screed shall be cast over it before erecting forms for footings.

##### All angles and corners, external or internal, shall be reinforced with an extra strip of 300 mm wide membrane sheet. The external and internal corners shall have “cut and cloaked” membrane pieces.

##### External corners shall have a minimum 20 mm chamfer.

##### Internal angles between the slab and walls shall be provided with a 40 x 40 mm preformed fillet.

##### In no case should the membrane be stretched at angles or corners. The membrane shall be dressed and eased around corners and angles.

##### At the location of pipes through the walls and floor slabs, reinforcing strips and collars shall be used.

##### For structures projecting above ground, the membrane shall be extended at least 150 mm above grade and terminated and finished in a 20 x 20 mm chase in the concrete. The chase shall be pointed immediately with bitumen flashing compound before backfilling.

###### instead of 20 x 20 mm chase, upon the Consultant's approval, aluminum flashing shall be used to secure the end of the exposed sheet waterproofing.

### Membrane shall be rolled out. Wrinkles and bubbles shall be minimized.

### Adhesive Bonded Membrane

#### The adhesive shall be applied according to the manufacturer’s instructions. The sheet shall be bonded to the substrate except those areas directly over or within 75 mm of a control or expansion joint.

### Mechanically Fastened Membrane

#### Mechanical fasteners shall be installed according to the manufacturer’s instructions. The sheet shall be bonded to membrane discs.

## FIELD QUALITY CONTROL

### General

#### The completed membrane shall be examined for defective or damaged areas before installing the protection course and shall be repaired or replaced according to the written instructions of the manufacturer.

### Flood Test

#### The Contractor shall provide temporary construction and materials for testing.

#### Before applying the protection layer, all horizontal applications shall be flood-tested with a minimum of 50 mm head of clean water for 72 hours.

#### If a leak is found, water shall be removed, and leaking areas shall be repaired with new waterproofing materials as the Consultant directs.

#### Flood testing shall be repeated. When the area is proven watertight, water shall be drained, and the dam shall be removed.

## CLEANING AND PROTECTION

### General

#### Areas with membrane shall be protected either with a screed or protection board at the end of a working day. No storage of materials or traffic shall be allowed in unprotected areas with waterproofing membranes.

### All below-ground membrane surfaces shall be protected with protection boards before backfilling operations can begin.

### On horizontal surfaces with membrane, where reinforcing steel is to be placed, a 25 mm thick layer of sand/cement screed shall be cast. Placing of formworks, reinforcements, and concrete shall begin after the screed has sufficiently hardened. Other membrane protection materials, instead of screed, may be used provided the Consultant's approval is obtained.

### Care shall be exercised during the backfilling operations so as not to dislocate the protection board and damage the membrane.

### Clean spillage and soiling from adjacent construction using cleaning agents and procedures recommended by the manufacturer of affected construction.

# END OF SECTION